| Product name | Silicone printing paste |
| --- | --- |
| State | Paste |
| Packing | 25KG/drum for white, 20KG/drum for clear |
| Storage | 6 months in cool place |
| Application | Suitable for cotton, polyester etc |
| Features | 1. High elasticity 2. High fastness 3. High glossy 4. SGS detecting passed, no PVC, no heavy metal, no NPEOs |
| Mix proportion | Light: White printing paste 70-80% + Clear printing paste 20-30% + pigment ?% Deep: White printing paste 20-30% + Clear printing paste 70-80% + pigment ?% |
| Printing process | 1. Printing with clear printing paste for 1-2 times 2. Mixing with white printing paste, clear printing paste, pigment and stirring them evenly. 3. Printing for 3-4 times (3-4 scrapes per time). 4. Drying it in room temperature, or baking for 1-3 minutes under 150-180℃ 5. Finish. |
| Attentions |  |
| 品名 | 高光高弹性水性油墨硅胶浆 |
| 外观 | 糊状 |
| 包装 | 白胶浆25KG/桶，透明浆20KG/桶 |
| 贮存期 | 常温下12个月 |
| 应用 | 针织布，弹力布 |
| 卖点 | 1. 手感超柔软 2. 高弹性高亮度 3. 符合美国ASTM对邻苯二甲酸脂和欧盟EN71 Part 3对重金属含量的要求 |
| 调配比例 | 印浅色：白胶浆70-80% + 透明浆20-30% + 色种？% 印深色：白胶浆20-30% + 透明浆70-80% + 色种？% |
| 工艺流程 | 1. 丝网选用80-100目，用丝印硬方刀75度刮印, 以透明浆打底1-2次 2. 将白胶浆，透明浆，色种搅拌匀印2-3次 3. 24-48小时自然干燥，或150-180度焙烘1-3分钟 |
| 注意事项 |  |